Product Data Sheet

# Product Description & Main Application

Samic Maxima Ferrous LDF 10W40 API CF4 uses selected synthetic technology base oils and balanced additive system to deliver fuel economy performance, and to protect modern engines operating under extreme conditions of pressures and temperatures. It’s the ideal choice for operators of heavy-duty truck and bus fleets equipped with latest designs, including those with regulatory emission controlled & longer oil drain intervals, as well as satisfying the needs of older engines. It may be used in naturally aspirated and turbocharged diesel and petrol engines, providing excellent protection even under the most severe conditions.

# Performance & Customer Benefits

- Outstanding oxidation & thermal stability reduces sludge deposits and keeps the engine cleaner.

- Excellent fuel economy, due to its superior flow and frictional properties compared to conventional diesel engine oils.

- Excellent dispersancy & outstanding soot control during longer drain frequency (LDF) of engine oil.

- Extended TBN reserves provide improved acid neutralization and corrosion protection, which helps in extending oil drain intervals.

- It delivers excellent viscosity control, outstanding protection against wear and exceptional versatility featuring one oil for all fleet with multiple engines makes.

# Specifications & Recommendations

# Samic Maxima Ferrous LDF 10W40 API CF4 meets or exceeds following International and Builder specifications:

- API CF

- ACEA E7/E4

- MTU OIL Category 3

- MAN M 3277

- MB 228.5

- MACK EO-M plus

- Scania LDF-2

# Typical Physical Characteristics

| Samic Marvela Silver LDF | Test Method | Units | 10W-40 |
| --- | --- | --- | --- |
| Density @ 15 0C | ASTM D 4052 | gm/cc | 0.874 |
| Viscosity @ 100 0C | ASTM D 445 | cSt | 15.7 |
| Viscosity @ 40 0C | ASTM D 445 | cSt | 111 |
| Viscosity Index | ASTM D 2270 | - | 150 |
| Pour Point | ASTM D 97 | °C | -39 |
| Flash Point (COC) | ASTM D 92 | °C | 220 |
| Total Base Number | ASTM D 2896 | mg KOH/g | 15.8 |
| Sulfated Ash | ASTM D 874 | % wt | 1.1 |
| CCS Viscosity | ASTM D 5293 | cP | 6200 @ -25 °C |

The above figures are typical of blends with normal production tolerance and do not constitute a specification.

For further information, please contact: sales@Samiclubricants.com

# Text boxes

Samic Maxima Ferrous LDF 10W-40 API CF4

Extra High Performance Multigrade – Synthetic Blend Diesel Engine Oil