Product Data Sheet

Product Description & Main Application

Samic Dynamo 9000 SAE 50 CH-4 is high performance diesel engine oil formulated with highly refined base stocks and advanced technology additives to provide reliable performance in the latest emission designs, including those with EGR systems, as well as satisfying the needs of older engines. It may be used in naturally aspirated and turbocharged diesel and petrol engines, providing excellent protection even under the most strenuous conditions.

Performance & Customer Benefits

- Outstanding oxidation & thermal stability reduces sludge deposits and keeps the engine cleaner.

- Excellent engine protection by providing outstanding protection against wear.

- Improved fuel economy.

- Excellent dispersancy provides outstanding soot control in Exhaust Gas Recirculation (EGR) systems.

- Extended TBN reserves provide improved acid neutralization and corrosion protection, which helps in extending oil drain intervals.

Specifications & Recommendations

Samic Dynamo 9000 SAE 50 CH-4 meets or exceeds following International and Builder specifications:

- API CH-4, CG-4, CF-4, CF, SJ				•     Detroit Diesel 93K215

- ACEA E7/A3/B4 						•     CUMMINS CES 20076/7/20078

- CAT  ECF-1a, ECF-2					•     Deutz DQC –III-05

- MTU OIL Category 2 					•     Global DHD-1

- MAN M3275						•     MB 228.3/MB 229.1

- VOLVO VDS-3						•     MACK EO-N

- Renault VI RLD-2

Typical Physical Characteristics

| Samic Dynamo 9000 SAE | Test Method | Units | 50 |
| --- | --- | --- | --- |
| Density @ 15 0C | ASTM D 4052 | gm/cc | 0.890 |
| Viscosity @ 100 0C | ASTM D 445 | cSt | 20.2 |
| Viscosity @ 40 0C | ASTM D 445 | cSt | 234 |
| Viscosity Index | ASTM D 2270 | - | 99 |
| Pour Point | ASTM D 97 | °C | -21 |
| Flash Point (COC) | ASTM D 92 | °C | 236 |
| Total Base Number | ASTM D 2896 | mg KOH/g | 10.5 |
| Sulfated Ash | ASTM D 874 | % wt | 1.0 |

The above figures are typical of blends with normal production tolerance and do not constitute a specification.

For further information, please contact: sales@samiclubricants.com

# Text boxes

Samic Dynamo 9000 SAE 50 CH-4

High Performance Monograde Diesel Engine Oil