Product Data Sheet

Product Description

Samic Marvel Ivory 4T 10W40 SM is designed with high quality synthetic blend base stocks and advanced technology additive system to provide high level of protection and performance. It works harder than other conventional motor oils by continuously preventing dirt and sludge build-up and reduces engine noise. This product meets the requirements of most motorcycle manufacturers and is suitable for use in 4 stroke gasoline engines, naturally aspirated or turbo charged engines, operating in all round seasons and adapted to vehicles equipped with catalytic converters running on unleaded fuels.

Performance & Customer Benefits

- Excellent oxidation & thermal stability, helps in extending oil drain intervals.

- Very good shear stability and excellent viscosity temperature behavior.

- Superior protection against viscosity and thermal breakdown.

- Excellent detergency and dispersancy, reduces sludge formation which improves engine cleanliness.

- Superior sludge protection for greater engine reliability.

- Enhanced wear protection and improved engine cleanliness.

- Easier cold starts and improved fuel economy compared to mono-grade engine oils.

Specifications & Recommendations

Samic Marvel Ivory 4T 10W40 SM meets or exceeds following International and Builder specification:

- API  SM

- JASO MA 2

- JASO 4T Clutch performance

Main Application

Samic Marvel Ivory 4T is suitable for use in following:

- Motorcycle 4 Stroke gasoline engines.

- Naturally aspirated or turbo-charged engines.

Typical Physical Characteristics

| Samic Marvel Ivory 4T | Test Method | Units | 10W-40 |
| --- | --- | --- | --- |
| Density @ 15 0C | ASTM D 4052 | gm/cc | 0.870 |
| Viscosity @ 100 0C | ASTM D 445 | cSt | 14.30 |
| Viscosity @ 40 0C | ASTM D 445 | cSt | 95 |
| Viscosity Index | ASTM D 2270 | - | 155 |
| Pour Point | ASTM D 97 | °C | -36 |
| Flash Point (COC) | ASTM D 92 | °C | 230 |
| Total Base Number | ASTM D 2896 | mg KOH/g | 8.4 |
| Phosphorous | ASTM D 4951 | % wt | 0.098 |
| CCS Viscosity | ASTM D 5293 | cP | 5650 @ -25 °C |

The above figures are typical of blends with normal production tolerance and do not constitute a specification.

For further information, please contact: sales@samiclubricants.com

# Text boxes

Samic Marvel Ivory 4T 10W40 SM (JASO MA2)

Synthetic Blend Multigrade 4 Stroke Motorcycle Oil