Product Data Sheet

Product Description & Main Application

Samic Nova Silver CH-4 series diesel engine oil is formulated with high quality base stocks and specially selected additives to ensure optimum performance and protection for diesel engines requiring an API CH-4 specification. Suitable for modern and old diesel engines fitted on trucks, buses, construction or agricultural machinery with or without turbo charger, intercooler or sophisticated injection systems.

Performance & Customer Benefits

- Improved oxidation & thermal stability reduces sludge build up and keeps the engine cleaner.

- Excellent wear protection to extend engine efficiency and service life.

- Improved fuel economy, due to high fluidity at low temperatures.

- Reduced oil consumption.

- Improved resistance to deposit formation keeps engine clean to give your vehicle maximum power under extreme conditions.

- Enhanced TBN reserves provide improved acid neutralization and corrosion protection.

Specifications & Recommendations

Samic Nova Silver CH-4 series meets or exceeds following International and Builder specifications:

- API CH-4, CG-4, CF-4, CF, SL, SJ

- ACEA E7/A3/B4

- CAT ECF-1a

- MTU OIL Category-2

- MAN M3275

- MACK EO-M Plus

- VOLVO VDS-2

- CUMMINS CES 20076/7

- Deutz DQC –II-05

- Renault RD-2

- MB 228.3

Typical Physical Characteristics

| Samic Nova Silver | Test Method | Units | 20W-40 | 20W-50 |
| --- | --- | --- | --- | --- |
| Density @ 15 0C | ASTM D 4052 | gm/cc | 0.888 | 0.890 |
| Viscosity @ 100 0C | ASTM D 445 | cSt | 14.30 | 20.4 |
| Viscosity @ 40 0C | ASTM D 445 | cSt | 107 | 175 |
| Viscosity Index | ASTM D 2270 | - | 137 | 137 |
| Pour Point | ASTM D 97 | °C | -30 | -30 |
| Flash Point (COC) | ASTM D 92 | °C | 230 | 236 |
| Total Base Number | ASTM D 2896 | mg KOH/g | 10.0 | 10.0 |
| CCS Viscosity | ASTM D 5293 | cP | 6060 @ -15 °C | 6060 @ -15 °C |

The above figures are typical of blends with normal production tolerance and do not constitute a specification.

For further information, please contact: sales@samiclubricants.com

# Text boxes

Samic Nova Silver CH-4 series

High Performance Multigrade Diesel Engine Oil