Product Data Sheet

Product Description

Samic Syn Synchro HD GL-5 series is a range of high performance heavy duty gear oils, formulated from high quality Synthetic Blend of base oils and an advanced additive system. These lubricants are designed for automotive heavy-duty transmissions, axles and final drives.  Moreover these oils are specially engineered for heavy-duty axles and final drives where extreme pressures and shock loadings are expected.

Performance & Customer Benefits

- Exceptional thermal & oxidation stability protects against deposit formation and oil thickening, thus maintains the life and performance of lubricant and transmission.

- Outstanding anti-wear properties and excellent film strength provides exceptional equipment protection, that not only results in fewer breakdowns but also helps improve transmission efficiency.

- Excellent rust and corrosion protection for longer component life.

- Compatibility with seals and gaskets, leads to minimize oil leakage and reduced contamination.

Specifications & Recommendations

Samic Syn Synchro HD GL-5 series meets or exceeds following International and Builder specifications:

- API GL-5/MT-1 (eqv. MIL-L-2105D)	  •     MAN 342 M2

- SAE J2360					  •     ZF TE ML 05A, 7A, 12E, 16B, C & D, 17B, 19B, 21A

- Scania STO 1:0				  •     Volvo 1273.10

Main Application

Samic Syn Synchro HD GL-5 series is suitable for use in all Passenger cars, On-highway light and heavy duty trucks, and commercial vehicles.

- Suitable for Heavy duty manual transmissions, axles and final drives requiring API GL-5 level performance.

- Applications like Off-highway industries including: construction, mining, quarrying, and agriculture.

- Other heavy-duty industrial and automotive applications, involving hypoid gears operating under conditions where high speed/shock load, high speed/low torque, and/or low speed/high torque exists.

Typical Physical Characteristics

| Samic Syn Synchro HD | Test Method | Units | 75W80 | 75W90 |
| --- | --- | --- | --- | --- |
| Density @ 15 0C | ASTM D 4052 | gm/cc | 0.850 | 0.87 |
| Viscosity @ 40 0C | ASTM D 445 | cSt | 56.5 | 125 |
| Viscosity @ 100 0C | ASTM D 445 | cSt | 9.5 | 16.3 |
| Viscosity Index | ASTM D 2270 | - | 152 | 139 |
| Pour Point | ASTM D 97 | °C | -42 | -39 |
| Flash Point (COC) | ASTM D 92 | °C | 220 | 222 |
| Copper Strip Corrosion | ASTM D 130 | - | 1A | 1B |
| Foam Seq I,II,III | ASTM D 892 | ml/ml | 10/0 | 10/0 |
| Phosphorus | ASTM D 4951 | %wt | 0.055 | 0.055 |

The above figures are typical of blends with normal production tolerance and do not constitute a specification.

For further information, please contact: sales@samiclubricants.com

# Text boxes

Samic Syn Synchro HD 75W80, 75W90 GL-5

Synthetic Blend High Performance Manual Transmission Oil