Product Data Sheet

Product Description

Samic Syncro HD 80W140 GL-5 is a high performance heavy duty gear oil, formulated from high quality Synthetic Blend of base oils and an advanced additive system. These lubricants are designed for automotive heavy-duty transmissions, axles and final drives.  Moreover these oils are specially engineered for heavy-duty axles and final drives where extreme pressures and shock loadings are expected.

Performance & Customer Benefits

- Exceptional thermal & oxidation stability protects against deposit formation and oil thickening, thus maintains the life and performance of lubricant and transmission.

- Outstanding anti-wear properties and excellent film strength provides exceptional equipment protection, that not only results in fewer breakdowns but also helps improve transmission efficiency.

- Excellent rust and corrosion protection for longer component life.

- Compatibility with seals and gaskets, leads to minimize oil leakage and reduced contamination.

Specifications & Recommendations

Samic Syncro HD meets or exceeds following International and Builder specifications:

- API GL-5					  •     MAN 342 M1/M2

- MIL-L-2105D (U.S Military Specification)	  •     ZF TE-ML 05A/7A/12E/16B,C&D/17B/19B/21A

- Scania STO 1:0				  •     Volvo 1273.10

Main Application

Samic Syncro HD 80W140 GL-5 is suitable for use in all Passenger cars, On-highway light and heavy duty trucks, and commercial vehicles.

- Suitable for Heavy duty manual transmissions, axles and final drives requiring API GL-5 level performance.

- Applications like Off-highway industries including: construction, mining, quarrying, and agriculture.

- Other heavy-duty industrial and automotive applications, involving hypoid gears operating under conditions where high speed/shock load, high speed/low torque, and/or low speed/high torque exists.

Typical Physical Characteristics

| Samic Syncro HD | Test Method | Units | 80W140 |
| --- | --- | --- | --- |
| Density @ 15 0C | ASTM D 4052 | gm/cc | 0.89 |
| Viscosity @ 40 0C | ASTM D 445 | cSt | 254 |
| Viscosity @ 100 0C | ASTM D 445 | cSt | 25.6 |
| Viscosity Index | ASTM D 2270 | - | 130 |
| Pour Point | ASTM D 97 | °C | -33 |
| Flash Point (COC) | ASTM D 92 | °C | 242 |
| Copper Strip Corrosion | ASTM D 130 | - | 1B |
| Foam Seq I,II,III | ASTM D 892 | ml/ml | 20/0 |
| Phosphorus | ASTM D 4951 | %wt | 0.055 |

The above figures are typical of blends with normal production tolerance and do not constitute a specification.

For further information, please contact: sales@samiclubricants.com

# Text boxes

Samic Syncro HD 80W140 GL-5

Synthetic Blend High Performance Manual Transmission Oil